## Slide 1
2022.05.19
Ju Ho Lee, Sun Seok Hong, Jae-Won Lee,
Yung-Zun Cho and Jong Kwang Lee
Korea Atomic Energy Research Institute
Preliminary Study for Oxidative Decladding
of Simulated Damaged Spent Fuel
Held in Vertical Position
www.kaeri.re.kr

## Slide 2: Stabilization of damaged used nuclear fuel
Damaged Spent Nuclear Fuel(SNF)
  No internationally accepted definition of “damaged fuel”
  Any SNF that requires non-standard handling to demonstrate compliance with applicable safety, regulatory or operation requirements* (Fuel with cladding defects greater than hairline cracks or pinholes, in USA)
  Pinholes, hairline cracks, through-wall cracks, debris
Handling Technology for Damaged SNF
  Repackaging technology(Encapsulation/Canning) mainly being considered for effective treatment for damaged SNF
  However, in long-term storage and final disposal of damaged SNF, potential risk due to moisture not completely removed in repackaging technology
   Recycling technology as Ultimate solution for
  Damaged SNF management
*Management of Damaged Spent Nuclear Fuel, IAEA Nuclear Energy Series
< ORANO technology>

## Slide 3: Concepts of stabilizing technology
Recovering fuels
as U3O8 powder
from damaged SNF
Fabrication of the stabilized pellet
Improvements
of U3O8 powder
Fabrication of stabilized fuel rod
Management
of stabilized fuel rod
Safeguards
Key 1 process
Key 2 process
Key 3 process
Milling or
Oxidation-Reduction Cycles
Compaction
Sintering

## Slide 4: Suitable decladding method to Damaged SNF
< 누출연료봉 >
< 손상연료봉 >
< 지지격자-연료봉 프레팅 >
< 이물질 프레팅 >
Mechanical Decladding
Mechanically separation of pellet and cladding by passing rod-cut through slitting module
Not applicable to Damaged SNF due to defect and flaws in cladding
Oxidative Decladding
Separation of pellet and cladding by volume expansion effect of UO2 oxidation leading to U3O8 pulverization
Not affected by defect and flaws in cladding of damaged SNF
X

## Slide 5: Motivation
Preliminary study for Derivation of Oxidation condition for KAERI Oxidative Decladding equipment
    Feasibility Study of oxidative decladding for 20 cm rod
    Evaluation of the time required for completely oxidation for 20 cm
    Optimal Condition for reduced oxidation time
20 cm
0.8 cm
< Schematic drawing of KAERI
oxidative decaldding equipment>
< Decladding Concept >
Vertical
vibration
Oxidant
U3O8
powders

## Slide 6: Previous study of KAERI (I)
Vertical Oxidative Decladding Experiment for SF rod-cut at 2009
    Decreased decladding efficiency for high-burnup rod-cut
    No complete decladding for rodcut of length higher than 30 mm
0.8 cm
Jeong-Won Lee, KAERI/RR-3131/2009

## Slide 7: Previous study of KAERI (II)
Vertical Oxidative Decladding Experiment for SF rod-cut at 2014
    Powders released from upper part of rod-cut
0.8 cm

## Slide 8: Preparation of simulated Damaged Fuel Rod
<Equipment for fabricating simulated spent-fuel rod >
<Cross-section of simulated SNF>
<Simulated SNF of different sizes>
Ar
Ar
Ar
Heat
HIP(Hot Isostatic Pressing) based equipment
    Thermal treatment under argon atmosphere at 1000oC and 70 bar during 30 min
<Chemical bonding between UO2 and cladding>

## Slide 9: Lab-Scale Equipments for oxidative decladding
저울
Balance
Air vibrator
Heater
Weighing balance at bottom
 Evaluation of Real-time Oxidation behavior

## Slide 10: Test # 1 : Oxidation of 10 cm Rodcut (Ar → 100% O2, 520oC)
*ASME Boiler and Pressure Vessel Code – Section III Division 5, 2021
Upper Side : Powderization observed
Bottom Side : Rupture in cladding Resulted from Rapid oxidation rate
<Upper Side of Oxidized Rod-cut>
Evaluation of Gas Change Effect on Oxidative Decladding
    Thermal treatment under argon atmosphere at 1000oC and 70 bar during 30 min
<Bottom Side of Oxidized Rod-cut>

## Slide 11: Test # 2 : Oxidation of 5 cm Rodcut (Air, 528oC)
*ASME Boiler and Pressure Vessel Code – Section III Division 5, 2021
Before After
Oxidation Oxidation
It tooks 6 hours for completely decladding 5 cm rod-cut
Decladding rate of 0.072 g UO2/min

## Slide 12: Test # 3 : Oxidation of 5 cm Rodcut (100 % O2 , 475 oC)
After Air After O2
Oxidation Oxidation
100 minutes oxidation time for completely decladding 5cm rod-cut
Compared to air oxidation, 70 % in oxidation
time reduced

## Slide 13: Test # 4 : Oxidation of 10 cm Rodcut (100% O2, 475 oC)
Incomplete Decladding (89%)
Rupture in cladding dut to volume expansion
`
`
6 cm
2 cm

## Slide 14: Optimal Oxidative Decladding Condition
Temperature(oC)
Oxygen Content
Higher Oxidation Rate
Rupture in Cladding
Intermediate Oxidation Rate
leading to no Rupture
For complete decladding of 20-cm rodcut, Rupture in cladding should be avoided
    Decladding rate (or Oxidation rate) should be adjusted
    100% O2 gas is not favored in oxidative decladding

## Slide 15: Concept for oxidative decladding equipment for HFEF
Air vibrator # 1
Heater
Air vibrator # 2
Air vibrator # 1
Air vibrator # 2
U3O8 powder
Oxidative Decladding mode
Air vibrator # 1
Air vibrator # 2
UO2 powder
Reduction-Oxidation mode
Air or O2
4% H2/Ar

## Slide 16: Conclusion
Higher Oxygen content and high temperature results in increased decladding rate, however, volume expansion in cladding was also observed due to either rapid oxygen penetration or increased local temperature associated with exothermic reaction of UO2 with oxygen
For complete decladding, rapid volume expansion in cladding should be avoided and thus oxygen content less than 100% is recommended for optimal decladding condition (Temp around 500oC and Oxygen content ranging from 20% to 80%)
Vibration effect was found to induce powder release from cladding : Vertical vibration more effective in powder release than Horizontal vibration